## Slide 1: HADEED PCCP PIPELINE CP SYSTEM UPGRADING A CASE STUDY
AbdulHameed Akeel
Staff Civil Engineer
Specialty Maintenance Dept.
Saudi Iron & Steel Company (HADEED)

## Slide 2: BACKGROUND
DESCRIPTION OF PIPELINE
2 SUPPLY LINES FROM INTAKE CHAMBER-KSA1 TO SEA WATER STATION - KSA3, 750 M LONG, 2,000 mm DIA. AWWA C301 PIPES
2 RETURN LINES FROM OUTFALL CHAMBER-KSA3 TO KSA2, 797 M LONG, 2,000 mm DIA. AWWA C301 PIPES
DEPTH OF TOP OF PIPES AT ABOUT 2 M FROM GL
PIPES PARTIALLY BELOW WATER TABLE

## Slide 3: BACKGROUND
DESCRIPTION OF EXISTING CP SYSTEM
ICCP SYSTEM WITH DISCRETE HIGH SILICON IRON ANODES INSTALLED AT DEPTHS BELOW WATER TABLE
COMMON TRs WITH CONCRETE CHAMBERS KSA1, KSA2 & KSA3
NO REs WERE INSTALLED ALONG THE PIPELINE
ONLY 2 REs WERE INSTALLED AT KSA3 CLOSE TO THE PIPES BUT NOT ON THE PIPE SURFACE

## Slide 4: BACKGROUND
ANTICIPATED PROBLEMS
AS NO REs WERE INSTALLED ON SURFACE OF THE PIPES, CP SYSTEM FOR PIPES COULD NOT BE MONITORED
AS TRs WERE COMMON WITH CONCRETE CHAMBERS, NO ADJUSTMENT COULD BE MADE TO CONTROL THE PROTECTION CURRENT TO THE PIPES
PIPES COULD HAVE BEEN OVER-PROTECTED, WHICH IS NOT GOOD FOR PCCP

## Slide 5: SCOPE OF UPGRADING WORK
PHASE 1-ASSESSMENT
EXPOSING PIPES AT 2 LOCATIONS AND ASSESSING THE CONDITION
INSTALLING REs ON SURFACE OF THE PIPES AT 3, 9 & 12 O CLOCK POSITIONS AND MEASURE POTENTIALS
PHASE 2-UPGRADING
ISOLATE ELECTRICALLY PIPES FROM CONCRETE CHAMBERS
INSTALL NEW TRs TO POWER THE ANODES PROTECTING THE PIPELINES
INSTALL REs AND INs ALONG THE PIPELINE AT REGULAR INTERVALS
ADJUST PROTECTION CURRENT TO MEET SABIC CP PROTECTION CRITERIA

## Slide 6: PHASE 1 FINDINGS
PIPES WERE FOUND TO BE COATED WITH BLACK EPOXY COATING AND WERE IN GOOD CONDITION
PIPE JOINTS WERE IN GOOD CONDITION (4 JOINTS WERE EXPOSED)
PRESTRESSING WIRES WERE EXPOSED AT 8 LOCATIONS AND ALL WERE IN GOOD CONDITION WITH BRIGHT STEEL
REs AT 3 & 9 O CLOCK POSITIONS SHOWED OVER-PROTECTION (NEGATIVE IO POTENTIALS MORE THAN 900 mV) AND RE AT 12 O CLOCK POSITION UNDER-PROTECTED

## Slide 7: PHASE 1 FINDINGS
PIPE SURFACE, COATING & PRESTRESS STEEL IN GOOD CONDITION

## Slide 8: PHASE 1 FINDINGS
SN INSTALLATION

## Slide 9: PHASE 1 FINDINGS
RE INSTALLATION

## Slide 10: PHASE 1 FINDINGS
Excavation Location No. | Pipe | Reference Electrode No. | Reference Electrode Location | On Potential (mV) | Instant Off Potential (mV) | After 24 hrs | 
 |  |  |  |  |  | Off Potential (mV) | Decay (mV)
1 | South South South | RE1 | 12 O’ clock | -1074 | -1027 | -818 | 209
 |  | RE2 | 3 O’ clock | -1191 | -1068 | -895 | 173
 |  | RE3 | 9 O’ clock | -1160 | -1046 | -913 | 133
1 | North North North | RE4 | 12 O’ clock | -965 | -883 | -501 | 382
 |  | RE5 | 3 O’ clock | -1322 | -1066 | -911 | 155
 |  | RE6 | 9 O’ clock | -1181 | -1069 | -918 | 151
2 | South South South | RE1 | 12 O’ clock | -1219 | -1137 | -1084 | 53
 |  | RE2 | 3 O’ clock | -1161 | -1024 | -966 | 58
 |  | RE3 | 9 O’ clock | -1193 | -992 | -922 | 70
2 | North North North | RE4 | 12 O’ clock | -1135 | -1017 | -953 | 64
 |  | RE5 | 3 O’ clock | -1252 | -1044 | -966 | 78
 |  | RE6 | 9 O’ clock | -1207 | -1155 | -1070 | 85

## Slide 11: PHASE 2
LOCATION OF NEW TRs AND JBs

## Slide 12: PHASE 2
LOCATION OF EXISTING ANODES AND NEW REs, INs & SNs

## Slide 13: PHASE 2
RE, IN & SN LOCATION

## Slide 14: PHASE 2
RE, SN & IN DETAIL

## Slide 15: PHASE 2
RE & IN INSTALLATION (AT TOP, JUST ABOVE & JUST BELOW GWT)
1. Concrete chipped out and RE placed close to prestressing steel

## Slide 16: PHASE 2
ENCAPSULATION OF Res IN CEMENT MORTAR (AT TOP, JUST ABOVE & JUST BELOW GWT)
2. RE enclosed in cement mortar

## Slide 17: PHASE 2
INSTALLING SN & IN CONNECTION TO STEEL CYLINDER
1. Hole drilled up to steel cylinder and Titanium Rod inserted

## Slide 18: PHASE 2
INSTALLING SN & IN CONNECTION TO STEEL CYLINDER
2. Titanium Rod welded to steel cylinder by cad welding

## Slide 19: PHASE 2
INSTALLING SN & IN CONNECTION TO STEEL CYLINDER
3. Continuity checked between two connections

## Slide 20: PHASE 2
INSTALLING SN & IN CONNECTION TO STEEL CYLINDER
4. Cables crimped to Titanium Rod by crimping & enclosed in heat shrink sleeve

## Slide 21: PHASE 2 FINDINGS
PROTECTION CURRENT FOR PIPES CAN BE ADJUSTED
PIPES CAN BE MONITORED BY MEASURING POTENTIALS OF THE PERMANENT Res
POTENTIALS WERE MONITORED BY THE INSTALLATION CONTRACTOR QUARTERLY FOR ONE YEAR
POTENTIALS WERE FOUND TO BE WITHIN THE SABIC CRITERIA RANGE (-720 TO -900 Mv ; 100 Mv Decay Potential in 24 hrs)

## Slide 22: PHASE 2 FINDINGS
  Seawater Prestressed Concrete Pipelines – Supply Pipeline
Zone 1
TR & Channel No.: TR 8, Channel 2
TR channel rating: 25 V, 50 A
TR channel operating: 7.02 V, 9.33 A
No. of REs: 12
No. of REs meeting protection criteria: 12 (100%)
Zone 2
TR & Channel No.: TR 9, Channel 2
TR channel rating: 25 V, 50 A
TR channel operating: 4.45 V, 3.31 A
No. of REs: 9
No. of REs meeting protection criteria: 9 (100%)

## Slide 23: PHASE 2 FINDINGS
  Seawater Prestressed Concrete Pipelines – Return Pipeline
Zone 1
TR & Channel No.: TR 8, Channel 1
TR channel rating: 25 V, 50 A
TR channel operating: 6.6 V, 11.02 A
No. of REs: 18
No. of REs meeting protection criteria: 18 (100%)
Zone 2
TR & Channel No.: TR 9, Channel 1
TR channel rating: 25 V, 50 A
TR channel operating: 4.39 V, 3.29 A
No. of REs: 15
No. of REs meeting protection criteria: 15 (100%)

## Slide 24: PHASE 2 FINDINGS
MONITORING DATA FOR SUPPLYN PIPELINE (ZONE 2)
Location : |  | Zone-2 SW pipeline |  |  |  |  |  |  |  |  |  |  |  | 
Time |  |  |  |  |  |  | Depolarization Potential |  |  |  | Decay Potential |  |  | 
Junction Box | Zone No. | Reference Electrode No. | Structure Connection (IN) No. | Base Potential (mV) | ON Potential (mV) | Instant OFF (mV) |  |  | 24Hrs |  |  | 24Hrs |  | Remarks
MMJB2 | SP-2 | RE-SP2-1 | JB-19-IN | -518 | -755 | -743 |  |  | -583 |  |  | 160 |  | P
 |  | RE-SP2-2 | " | -510 | -763 | -751 |  |  | -588 |  |  | 163 |  | P
 |  | RE-SP2-3 | " | -535 | -779 | -769 |  |  | -597 |  |  | 172 |  | P
 |  | RE-SP2-4 | JB-20-IN | -280 | -525 | -513 |  |  | -411 |  |  | 102 |  | P
 |  | RE-SP2-5 | " | -266 | -790 | -781 |  |  | -724 |  |  | 57 |  | P
 |  | RE-SP2-6 | " | -540 | -730 | -724 |  |  | -658 |  |  | 66 |  | P
 |  | RE-SP2-7 | JB-21-IN | -785 | -952 | -948 |  |  | -927 |  |  | 21 |  | P
 |  | RE-SP2-8 | " | -799 | -921 | -918 |  |  | -892 |  |  | 26 |  | P
 |  | RE-SP2-9 | " | -460 | -774 | -766 |  |  | -719 |  |  | 47 |  | P
Notes: DGB- Deep Buried Ground Zone, GLB- Grade Level Buried Zone & A - Atmospheric Zone, NS- Not Stable |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Remarks : Current is not increasing by potentiometer more 3.31A |  |  |  |  |  |  |  |  |  |  |  |  |  | 
As found | CH2- 4.48V, 3.28A, 4.11mV, Shunt rating-60A=75mV (0.8mV) |  |  |  |  |  | As left | CH2- 4.45V, 3.31A, 4.14mV |  |  |  |  |  | 

## Slide 25: PHASE 2 FINDINGS
MONITORING DATA FOR RETURN PIPELINE (ZONE 2)
Location : |  | Zone-2 SW pipeline |  |  |  |  |  |  |  |  |  |  |  | 
Time |  |  |  |  |  |  | Depolarization Potential |  |  |  | Decay Potential |  |  | 
Junction Box | Zone No. | Reference Electrode No. | Structure Connection (IN) No. | Base Potential (mV) | ON Potential (mV) | Instant OFF (mV) |  |  | 24Hrs |  |  | 24Hrs |  | Remarks
MMJB2 | RP-2 | RE-RP2-1 | JB-10-IN | -561 | -853 | -834 |  |  | -629 |  |  | 205 |  | P
 |  | RE-RP2-2 | " | -554 | -841 | -821 |  |  | -617 |  |  | 204 |  | P
 |  | RE-RP2-3 | " | -529 | -826 | -815 |  |  | -606 |  |  | 209 |  | P
 |  | RE-RP2-4 | JB-11-IN | -550 | -785 | -769 |  |  | -608 |  |  | 161 |  | P
 |  | RE-RP2-5 | " | -577 | -791 | -767 |  |  | -610 |  |  | 157 |  | P
 |  | RE-RP2-6 | " | NS | -804 | -794 |  |  | -626 |  |  | 168 |  | P
 |  | RE-RP2-7 | JB-12-IN | -584 | -759 | -737 |  |  | -618 |  |  | 119 |  | P
 |  | RE-RP2-8 | " | -543 | -738 | -726 |  |  | -600 |  |  | 126 |  | P
 |  | RE-RP2-9 | " | -567 | -760 | -757 |  |  | -622 |  |  | 135 |  | P
 |  | RE-RP2-10 | JB-13-IN | -573 | -793 | -765 |  |  | -647 |  |  | 118 |  | P
 |  | RE-RP2-11 | " | -578 | -807 | -797 |  |  | -651 |  |  | 146 |  | P
 |  | RE-RP2-12 | " | -512 | -817 | -807 |  |  | -643 |  |  | 164 |  | P
 |  | RE-RP2-13 | JB-14-IN | -561 | -798 | -775 |  |  | -634 |  |  | 141 |  | P
 |  | RE-RP2-14 | " | -578 | -834 | -812 |  |  | -648 |  |  | 164 |  | P
 |  | RE-RP2-15 | " | -582 | -837 | -816 |  |  | -644 |  |  | 172 |  | P
Notes: DGB- Deep Buried Ground Zone, GLB- Grade Level Buried Zone & A - Atmospheric Zone, NS- Not Stable |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Remarks : |  |  |  |  |  |  |  |  |  |  |  |  |  | 
As found | CH1- 3.98V, 2.68A, 3.36mV, Shunt rating-60A=75mV (0.8mV) |  |  |  |  |  | As left | CH1- 4.39V, 3.29A, 4.12mV |  |  |  |  |  | 

## Slide 26: CONCLUSIONS
CONDITION OF EXISTING SEAWATER PCCP PIPELINES UNDER ICCP WERE INSPECTED TO CHECK THEIR CONDITION AND FOUND IN GOOD CONDITION.
EXISTING CP SYSTEM WAS COMMON WITH SEAWATER CHAMBERS AND ADJUSTMENT OF PROTECTION CURRENT WAS NOT POSSIBLE.
EXISTING CP SYSTEM HAD NO MONITORING SYSTEM (NO REs WERE INSTALLED).

## Slide 27: CONCLUSIONS
EXISTING CP SYSTEM UPGRADED BY
INSTALLING SEPARATE TRs FOR THE PCCP
INSTALLING REs AND INs ALONG THE LENGTH OF THE PIPES AT TOP, 9 O CLOCK (JUST ABOVE WT) & 9 O CLOCK (JUST BELOW WT)
CP SYSTEM CAN NOW BE ADJUSTED INDEPENDENTLY AND OVER-PROTECTION AVOIDED.
AFTER UPGRADING, THE INSTANT OFF POTENTIALS WERE WITHIN SABIC PROTECTION CRITERIA i.e. -720 mV TO -900 mV.