## Slide 1: Morgan Advanced Materials Thermal Product Division
Pipe Insulation
A Thermal Engineering Approach
JUBCOR- 2018
Al-Jubail

## Slide 2
Head Office in Windsor, UK and listed on the LSE (FTSE 250)
160+ years of continuous trading
Operate in 50+ countries
We do business the right way, ethically and safely
£1,021.5M total global sales
Selling into 100 countries
Manufacturing in 30 countries
Approximately 8,900 employees
Morgan Advanced Materials -
a global engineering company
Our structure
Thermal Products
Division
Carbon and Technical
Ceramics Division
Thermal Ceramics
Electrical Carbon
Molten Metal Systems
Seals and Bearings
Technical Ceramics
Composites & Defence Systems
We work in the electronics, energy, healthcare, industrial, petrochemical, security and transport markets, forming close collaborative relationships with our customers

## Slide 3
Thermal Ceramics offers a range of thermal management solutions with an extensive range of high temperature insulation systems and products and for thermal insulation in high-temperature environments. Insulating fibre, bricks and monolithics account for 42% of Morgan Group revenue in 2017.
Our products are used to reduce energy consumption in industrial processes and provide fire protection.
Our products are renowned to help customers, especially those operating energy-intensive processes, to reduce energy consumption, emissions and operating costs.
36 manufacturing sites spread across 5 continents, manufacturing fibre, bricks, monolithics and microporous products.
An introduction to Thermal Ceramics

## Slide 4
16/01/2015
90
£ 1,021.5M
TOTAL GLOBAL SALES
﻿OVER 85 MANUFACTURING SITES
MANUFACTURING IN 30 COUNTRIES
SELLING INTO 100 COUNTRIES
APPROXIMATELY 8,900 EMPLOYEES
Our Global presence

## Slide 5
Our
Global
Thermal
Ceramics
Footprint
09/10/2017
Morgan Advanced Materials Commercial Information
9

## Slide 6: CUI – Corrosion Under Insulation
Substantial researches and facts reveal:
CUI is commonly seen in the pipes at the temp range of -4 ~350℃;
The primary reason of CUI is the moisture absorption of insulation.
It is difficult to estimate where CUI takes place and there is very limited method to make detection;
Corrosion takes place amazingly fast;
Huge loss is caused by regular maintenance and irregular maintenance;
CUI is the primary cause of pressure decrease, temp change, pipe damage and leakage, and safety incident.

## Slide 7: What Features are mainly requested?
Industrial
Moisture prevention (Preventing CUI or resistance to CUI, resistance to water)
Corrosion resistance (Chloride content as reaction to austenitic stainless steel (corrosion).
Maintain temperature difference along the pipe run.
Maintain/control heat flow rate.
Handleable – low dust, not fragile, minimal free fiber irritation
Resistance to impact (Walking through resistance).
Limited maintenance, ease of repairing.
Pipe congestion.
Carbon footprint (as result of poor management insulation)
Energy saving by maximizing process control and reducing heat losses.

## Slide 8: CUI - Prevention - Morgan solutions
Microporous Insulation
Hydrophobic (through the mix) – breathable against moisture
Water repellent (through encapsulation) – aluminium barrier (600C)
Superwool Plus Blanket
Hydrophobic – breathable against moisture.
Leachable Chloride according to ASTM C 871 - Below 10 ppm

## Slide 9: Product utilization in hot piping insulation
Materials in % (quantity) | Process piping |  |  | Transport piping
Temperature range | 250 to 450°C | up to 650°C | 1000°C (heaters) | 
Stone fibers | 28% | 40% | - | 30%
Foamglass | 25% | - | - | 20%
Casi and Perlite | 15% | 25% | 34% | 10%
other fibers incl glass | 25% | 30% | 65% Only HT fibers | 20%
MP and aerogel | 10% |  | 1% | 5%
Glass beads | - | - | - | -
Foams (PU, etc) | 5% | - | - | 15%
Piping insulation (mechanical insulation) is generally combined with the delivery of the cladding +installation in situ.
Fibers (mineral wool) followed by calcium silicate have a predominant portion of the market but tendency is to find more reliable alternatives (pedestrian resistance, CUI, stability over time, H&S, energy saving, cladding and installation time savings)
Coatings are more and more often they are complementary to ‘solid’ insulation as being part of a system (same as cladding)

## Slide 10: Insulation thickness by product - Examples
ID 200 mm
600°C
30 mm WDS Microporous (Shell)
1 layer
OD = 260 mm
Cladding x linmt = 0,816 m2
110 mm Calcium SIlicate
OD = 420 mm
Cladding x linmt = 1,412 m2
10 mm WDS Microporous (Flexible)
30 mm SW (hydrophobic grade)
OD = 340 mm
Cladding x linmt = 1,067 m2
125 mm Mineral Wool
OD = 450 mm
Cladding x linmt = 1,444 m2
50 mm Aerogel Blanket
5 layers
OD = 300 mm
Cladding x linmt = 0,942 m2

## Slide 11: Pipe Insulation in O&G - Value Proposition
Value Proposition: Morgan have developed an innovative concept that comprises Microporous + Superwool Plus blankets that can delivers:
Time saving (faster installation than blankets or matresses products)
Reduce CUI (corrosion under insulation) through the use of a coating instead of metal cladding and water repellent products.
Save space (decreasing pipe rack density) due to the exceptional low thermal conductivity of microporous.
Energy saving by maximizing process control and reducing heat losses.
Notable saving in metal cladding expenditure (thinner insulation = smaller pipe diameter)

## Slide 12: Pipe Insulation – Superwool Plus Blanket

## Slide 13: Pipe Insulation – Comparison of
Superwool + WDS
WDS Shell
Mineral Wool

## Slide 14: Example of optimization on pipe racks density and space
Insulation | Microporous Insulation | Conventional Insulation
Pipe ID: 50mm Working space increased by 56% |  | 
Pipe ID: 150mm Working space increased by 44% |  | 
Pipe ID: 300mm Working space increased by 28% |  | 
530mm
370mm
260mm
210mm
135mm
410mm
50mm
*pipe gap: 50mm

## Slide 15: Pipe Rack – Space Optimization

## Slide 16: Pipe rack congestion – Space optimization
Larger space available between a pipe an another facilitates access for ease maintenance
Higher number of pipeline can be installed in the same space

## Slide 17: Pipe Insulation – Cost Saving on Cladding
Less Cladding is required with notable cost saving

## Slide 18: Superwool Plus Blankets VS Mineral Wool
Features | Superwool Plus | Mineral Wool
Temperature | 1200C | 700C
Fiber Index | Improved insulation up to 30% vs conventional fibers | -
 | More fiber concentration | Efficient prevention of heat transfer through convection and greater strength
Unfiberized particles (shot) | Reduced mechanical skin irritation | Irritating to skin, abrasive.
Mechanical Properties | Excellent tensile strength | Limited
H&S | Low bio-persistence according to nota Q of EU Directive | potentially carcinogenic, not low bio-persistent
Non combustibility | 100% Inorganic - Non combustible, no burnout, no gas emission Properties are maintained up to the maximum using temperature | contains organic binders witch burns from 80C to 200C approx.
Vibration resistance | Stitching producing method | Poor vibration resistance once the binders are burn – sagging phenomena
Pedestrian resistance | Very high resiliency | Poor

## Slide 19: WDS® Microporous: a highly efficient insulation
Out-performing thermal conductivity in the widest temperature spectrum
Inorganic material, chemically inert
Non combustible
Thermally stable
Saves energy and facilitates exact calculations of heat losses
Reduces weight and volume in the insulation design
Recyclable and safe from an H&S perspective
1100ºC
2012ºF
-180ºC
-292ºF

## Slide 20: Why using WDS® Microporous Insulation ?
  To Optimize Space
  To Save Energy
  To Reduce Weight
To delivery premium valued solution for the customers :
Where size is a premium
Where space is limited
For Heat Flow control
For optimal Energy efficiency
Notes: This could be combined with Slide 14 and leave the detail on 14 up longer for more focus.

## Slide 21
WDS
Microporous
–
Best insulating properties
Thermal conductivity comparison of
WDS® microporous insulation products vs. other type of insulating materials
09/10/2017
Morgan Advanced Materials Commercial Information
26

## Slide 22: Pipe Clamp Support
WDS MultiFlex
To avoid thermal bridges and to reduce pipe support temperature

## Slide 23: Corrosion under insulation - Summary
Corrosion under insulation is a serious issue that many specifiers are very concerned with.
It is a complex issue as many combinations of factors affect it.
  Temperature pipe, ambient temperature, pipe material, materials in contact, weather, inside/out, Dew points, leaks, marine, chemical, insulation material, leachable, moisture resistance, moisture retention, inhibitors, cladding material, quality cladding application, damage to cladding, removal of cladding, sealing of cladding joints.
CUI can be solved only by careful designing of the insulation system and require more in depth analysis case by case.
For high temp piping insulation/CUI, Morgan firmly believe Superwool & Microporous insulation still provide the optimum solution in terms of performances, durability and ROI.

## Slide 24
Questions?
Thank You