## Slide 1: SMART COATING SELECTION METHODOLOGY (SCSM)
Kumar Kolur Vadivelu MICorr

## Slide 2
Alliance between Saudi Aramco and The Dow Chemical Company
The world's largest chemical complex ever built in a single phase
Twenty-six integrated world-scale manufacturing plants (14 are completely new to Saudi Arabia)
Sadara Chemical Company

## Slide 3: Why Coating Fails
Primary Causes | Failure Modes
Improper Surface Preparation Improper Coating Selection Improper Application Improper Drying, Curing and Over Coating times Lack of protection against water and aqueous system Mechanical Damage | Formulation – Related Failures Substrate – Related Failures Physical Defect – Related Failures

## Slide 4: Coating/Lining-Formulation Related Failures
Chalking
Erosion
Checking
Alligatoring
Cracking
Mud Cracking
Wrinkling
Biological Failure
Source: SSPC : Causes and Prevention of Paint Failure, Chap 23 Good Painting Practice, SSPC Manual, 1982.)

## Slide 5: Coating/Lining-Substrate Related Failures
Previously Used Steel
Galvanized or Metallic Zinc Surface
Aluminum
Copper
Wood
Concrete
Source: Federation of Societies for coating Technology, Philadelphia, PA. Pictorial standards of coating defects.)

## Slide 6: Coating/Lining-Physical Defect Related Failures
Blister
Craters
Orange Peel
Runs, Sags and Curtains
Paint Adhesion Loss
Solvent Popping, Boiling and Pinholes
Source: Industrial painting principles and practice, second edition , Norman Roobol , Hanser Gardner Publications, Cincinnati, OH,1997

## Slide 7: How To Prevent Coating Failures
Good Specifications
Good Design
Good Paint System
Good Application
Good Application Control and Inspection
This presentation focuses on basic things to be considered before selecting “SMART COATING”

## Slide 8: Learning Objectives
Primary Substrates for Application
Deciding on the Suitable Coating System
Application of Coating System
Quality Control and Assurance

## Slide 9: Nature of Primary Substrates
Nature of Primary Substrates
Underwater Structure
Piping System
Equipment
Vessel
Tanks
Above Ground Structure
Fixed Unit
Mobile Unit
Fixed Unit
Articulated Unit
Above Ground
Buried

## Slide 10: Primary Substrate – Environmental Consideration
Primary Substrate – Environmental Consideration
Atmospheric Condition
Immersion Condition
Buried (Soil) Condition

## Slide 11: Lifetime Expectancy of Primary Substrate
Lifetime Expectancy of Primary Substrate
Low Lifetime Structure
Medium Lifetime Structure
Long Lifetime Structure

## Slide 12: Primary Substrate - Functions
Primary Substrate - Functions
Structure
Piping System
Equipment
Storage
Production
Others

## Slide 13: Construction Material of Primary Substrate
Construction Material of Primary Substrate
Ferrous Metal
Non-Ferrous Metal
Carbon Steel
Cast Iron Steel
Stainless Steel
Duplex Steel
Aluminum
Galvanized Metals

## Slide 14: Expected Corrosion Hazard – Primary Substrate
Expected Corrosion Hazard – Primary Substrate
Dry Corrosion
Wet Corrosion

## Slide 15: Expected Thermal Impact – Primary Substrate
Expected Thermal Impact – Primary Substrate
Heating Effect
Cooling Effect
Burning
Expansion- Induced Cracks
Deterioration of Mechanical Properties
Flaking
Contraction-Induced Cracks
Deterioration of Mechanical Properties

## Slide 16: Primary Substrate – Contamination Hazard
Primary Substrate – Contamination Hazard
Chemical Contamination
Weather Contamination
Oil Spills
Chemical Spills
Sea Water Spray
Dust, Dirt
Rain
Humidity

## Slide 17: Primary Substrate – Ultraviolet Hazards
Primary Substrate – Ultraviolet Hazards
Sun Ray Effects

## Slide 18: Deciding the Suitable Coating System

## Slide 19: Coating Material – Desired Properties
Coating Material – Desired Properties
Barrier
Inhibitive
Galvanic

## Slide 20: Barrier Protection
The partial blocking of any or all elements by a semi-impermeable film Examples: Tank Linings, Ballast Tanks

## Slide 21: Inhibitive – Inhibition
Slowing Down the Corrosion Reaction by Passivation of the Substrate
Primers
Red Lead, Chromates

## Slide 22: Galvanic – Sacrificial
Pigment is anodic to the substrate and corrodes in preference to the steel.
Cathodic Protection
Most Common: Zinc-Rich Primers

## Slide 23: Coatings Materials – Classification
Coatings Materials – Classification
Organic Paints
Metallic
Inorganic Paints
Thermo Plastic
Elastomeric
Thermosetting
Zn Rich Coating
Hot Dipping Zn,Al,Pb
Electro Plating Ni,Cr,Zn,Sn,Cd
Thermally Sprayed Any Metal (Zn,Al,AL/Zn)
Cladding Stainless Steel
Conversion Coating
Cement Lining
Chromate
Phosphate
Anodize
Zinc Silicate
Portland
Pot. Silicate
Cal Aluminate
Modified Pot. Silicate

## Slide 24: Durability of Coating Material
Durability of Coating Material
Low Life Coating Material
Medium Life Coating Material
Long Life Coating Material

## Slide 25: Coating Material – Compatibility
Coating Material – Compatibility
Coating Layer Compatibility
Coating – Substrate Compatibility
Coating – Environmental Compatibility

## Slide 26: Coating Material Compliance Regulation/Standards (Client/Owner Req)
Coating Material Compliance Regulation/Standards (Client/Owner Req)
NACE – National Association of Corrosion Engineers
ACI – American Concrete Institute
SSPC – Steel Structural Painting Council
ICRI – International Concrete Repair Institute
ASTM – American Society for Testing and Materials
ISO – International Organization for Standardization
NORSK – Norwegian Technology Standard Institution

## Slide 27: Coating Material Specific – Health and Safety Requirements
Coating Material Specific – Health and Safety Requirements
In Service
During Application

## Slide 28: Coating Material – Cost Consideration
Coating Material – Cost Consideration
Cost of Painting Operation
Cost of Painting Test
Cost of Blasting Operation
Abrasive Material
Blasting Application
Painting Material
Painting Application
At Site
Lab

## Slide 29: Application of Coating System

## Slide 30: Surface Preparation
The majority of premature coating failures can be tied to surface preparation.

## Slide 31: Surface Preparation
Surface Preparation
Dry Abrasive Blasting
Open Blasting
Hand and Power Tool Preparation
Closed Blasting
Pickling
As Dictated by Vendor/Coating Mfg’er

## Slide 32: Preparation Standards
SSPC-SP1 | :Solvent Cleaning
SSPC-SP2 | :Hand Tool Cleaning
SSPC-SP3 | :Power Tool Cleaning
SSPC-SP5/NACE 1 | :White Metal Cleaning
SSPC-SP10/NACE 2 | :Near White Metal Cleaning
SSPC-SP6/NACE 3 | :Commercial Blast Cleaning
SSPC-SP7/NACE 4 | :Brush-off Blast Cleaning

## Slide 33: Preparation Standards (Cont.)
SSPC-SP12/NACE 5 | :Water Jetting Prior to Recoating
SSPC-SP13/NACE 6 | :Surface Preparation of Concrete
SSPC-SP14/NACE 8 | :Industrial Blast Cleaning
SSPC-SP15 | :Commercial Power Tool Cleaning
SSPC-SP11 | :Bare Metal Power Tool Cleaning

## Slide 34: Paint Application
Paint Application
Spray
Brush
Roller
As Dictated by Vendor/Coating Mfg’er
Airless Machine
Conventional Machine

## Slide 35: Quality Control and Assurance

## Slide 36: Method of Inspection
Method of Inspection
Inspection of Paint Material
Inspection of Coating Application
Inspection of Substrate
Inspection of Surface Preparation
Weather Condition, Coating Mixing/Thinning Wet Film Thickness Etc.,
Bare (Rust Grade)
Coated (Maintenance)
Cleanliness Degree
Roughness Degree

## Slide 37: Schedule of Inspection
Schedule of Inspection
Inspection Before Application
Inspection During Application
Inspection After Application

## Slide 38: Testing of Coating System
Testing of Coating System
Physical Testing
Chemical Testing
Coated Item Testing
Density Viscosity Etc.
Flashpoint Solid Content Pigment Types Etc.
Adhesion Hardness Flexibility Dry Film Thickness LV/HV Holiday
Testing
Etc.

## Slide 39
Conclusion
Prior to selecting smart coating, the following aspects about Material, Coating System, Application Technique and QA & QC program should be meticulously reviewed by qualified personnel.
Smart and effective coating selection success is based on cross-functional involvement and team effort.
Each aspect of process condition, including upset condition, should be considered prior to coating selection.
If any coating failure occurs, systematic RCI technique should be followed to rewrite an effective coating specification, to select smart coating that will survive intended service life.

## Slide 40
Thank you